## Slide 1: Tomorrow’s Castings
John Campbell
University of Birmingham UK
AFI Melbourne 2023

## Slide 2
Bottom gated laminar filling

## Slide 3
Top gated turbulent filling

## Slide 4: Turbulent Surface Entrainment Bifilms + Bubbles

## Slide 5
Surface Turbulence forming
Bifilm Cracks

## Slide 6
RPT Before and After Reduced Pressure

## Slide 7: Microstructure and Property Control by Bifilms

## Slide 8: aFe + bFe formed on bifilms

## Slide 10: The Origin of Fracture
Failure modes from Pre-Existing Cracks

## Slide 11
Theoretical Basis of Crack Formation
1920
Griffith: An Energy criterion
No specified geometry
1959
Barenblatt: A geometrical model
A region of zero cohesion edged by strong cohesion

## Slide 12
Tensile Properties

## Slide 13
Elongation and Yield Strength of A201/6

## Slide 14
Highly ductile Ni-base alloy CY40 tensile test piece
(with bifilms!)

## Slide 15
Al-Si alloy (Courtesy Zhu Zhang 2007).
Ductile Dimple Fracture

## Slide 16
Dendrite straightening of bifilms

## Slide 17: Fracture surfaces from parts of the same Al-4.5Cu alloy casting with and without an entrainment event

## Slide 18
Fatigue
A failure mode dominated by pre-existing cracks but only marginally by fatigue

## Slide 19
Wind Turbine Main Bearing
Fatigue Failure
Martin Evans et al 2012

## Slide 20
Bearing steel fatigue failure
Martin Evans et al 2012

## Slide 21
facet
Striations
Shear lips
Duraipandi, Babu and Moitra (2023). 316 Stainless Steel

## Slide 22
Compressor Failure
Sessna 208B
21 Jan 2006

## Slide 24
Creep
A failure mode due to stress at high temperature dominated by pre-existing cracks

## Slide 25
Creep of
Ni-Base Superalloy

## Slide 26
Stress Corrosion Cracking (SCC)
A failure mode due to corrodent penetration into pre-existing cracks. Opened by tensile stress.
Stopped by compressive stress.

## Slide 27
Hydrogen Embrittlement
+
Hydrogen Blistering
A failure mode from a
pre-existing crack population
1. Opened by pptn of inclusions, and
2. Pressurized by hydrogen.

## Slide 28: Cracked inclusion and associated crack
Inclusion
(Matrix)
Crack

## Slide 30
Stretched sheet 7475 (Al-Zn-Mg-Cu) Alloy
Heated to 515 C
in Air + NaBF4 in Air

## Slide 31
42CrMo4 Steel
(before and after 2h at 450C in hydrogen
at 19.5MPa pressure)
Courtesy E Martinez-Paneda 2022.

## Slide 32
Secondary Refining Processes

## Slide 33
Vacuum Induction Melting
VIM

## Slide 34
Electroslag Remelting
ESR
Vacuum Arc Remelting
VAR
Secondary Refining Processes

## Slide 35: Vacuum Arc Remelting (Dangerous Metallurgy)

## Slide 37
Build-up of VAR Ingot

## Slide 38
VAR
1

## Slide 39
Crack in VAR ingot
observed after salt bath heat treatment.
Peet & Bhadeshia 2017
60 mm

## Slide 40
VAR Historical Failures
1. Commercial Jets

## Slide 41
19 July 1989
United Airlines Flight 232
DC10 crash landed at Sioux City
Ti disc failure due to a hard alpha defect
112 Fatalities
Triple VAR
Hard defect fell out during forging

## Slide 42
United Airlines Flight 232
DC10 Sioux City 1989

## Slide 45
American Airlines 383 2016

## Slide 46
American Airlines 383 Ohare 2016

## Slide 47
ETCH PIT
(formed where bifilm intersects surface)
Image courtesy Metallurgical Associates Inc 2015

## Slide 48
VAR Historical Failures
2. Helicopters

## Slide 49
Year | Flight | Location | Helicopter Type | Fatalities | Cause
1977 | Service flight 451 | Norway Norwegian Sea | Eurocopter AS 332L1 Super Puma | 12 | Fatigue crack in the spline which caused the power transmission shaft to fail.
1978 | Service flight 165 | Norway North Sea | Sikorsky S-61 | 18 | Rotor blade loosened after fatigue to the knuckle joint
2009 | Service flight | North Sea | Super Puma | 14 | Gearbox failure
2012 May | Service flight | North Sea | Bond Super Puma Eurocopter EC255 | 0 | Gearbox cracks due to corrosion
2012 October | Service flight | North Sea | Bond Super Puma Eurocopter EC255 | 0 | Gearbox cracks due to corrosion
2016 | Service flight | Norway coast | Eurocopter EC255 | 13 | Fatigue of rotor shaft and loss of rotor
2018 | Military test | Korea | Marineon MUH-1 | 5 fatalities 1 injured | Fatigue of rotor shaft (plus defective Airbus spares)

## Slide 50
Atoms
1900
Strength,
Rigidity of Solids
A History of Metallurgy

## Slide 51
Atoms
1900
Strength,
Rigidity of Solids
A History of Metallurgy
Vacancies
1900
Point Defects
0-D
Diffusion

## Slide 52
Atoms
1900
Strength,
Rigidity of Solids
A History of Metallurgy
Vacancies
1900
Point Defects
0-D
Diffusion
Dislocations
1950
Line Defects
1-D
Plasticity

## Slide 53
Atoms
1900
Strength,
Rigidity of Solids
A History of Metallurgy
Vacancies
1900
Point Defects
0-D
Diffusion
Dislocations
1950
Line Defects
1-D
Control Plasticity
Bifilms
2000
Planar Defects
2-D
Control Fracture

## Slide 54: The End

## Slide 57
 | Liquid | Pb | Au | Nb | Pt | Pd | Hf | Ag | Al | Cu | Zr | Ti | Ni | Co | Fe | Mg | Mo | Nd | W | Re | Ir | Cr | Be
m/B | 0 | 0.12 | 0.15 | 0.22 | 0.22 | 0.23 | 0.27 | 0.29 | 0.35 | 0.35 | 0.39 | 0.42 | 0.43 | 0.45 | 0.48 | 0.49 | 0.48 | 0.50 | 0.52 | 0.54 | 0.56 | 0.72 | 1.42
n | 0.50 | 0.44 | 0.42 | 0.40 | 0.39 | 0.39 | 0.37 | 0.37 | 0.34 | 0.34 | 0.33 | 0.32 | 0.31 | 0.30 | 0.29 | 0.29 | 0.29 | 0.28 | 0.28 | 0.26 | 0.26 | 0.21 | 0.02
Ductile Brittle
The Ductile / Brittle Behaviour of Engineering Metals
m/B = Ratio of elastic modulus to bulk modulus
n = Poissons Ratio