## Slide 1: 10 Rules for Casting Applications in a Real World Environment
Australian Foundry Institute Conference 2023
Richard Seymour-Wright

## Slide 2: Content
Intro & Disclaimer!
The Ten Rules
Key Considerations for Casting Design
Case Studies
  Tanker Lid Casting – Gravity Die Casting – CA401 Aluminium
  Turbo Exhaust Collector Casting – Sand Casting - SiMo
  Base Casting – Sand Casting – Ni-Resist
Closing Summary & Questions

## Slide 3: Intro
Richard Seymour-Wright
  BEng (Phys Met)
  GDE (Ind Eng)
Disclaimer - No formal training or qualifications in methoding!!
Foundry IT (1998)
  Pro/Engineer
  AFSolid – now SolidCAST / FlowCAST / OptiCast
“Technical Manager” – Alliance Connect
  Since 2017
  Responsible for New Product Development & Casting Processes (~50%)

## Slide 4: The 10 Rules
Achieve a good quality melt
Avoid turbulent entrainment (critical velocity)
Avoid laminar entrainment of the surface film (no stopping / reversal of flow)
Avoid bubble damage
Avoid core blows (core venting)
Avoid shrinkage damage (7 feeding rules)
Avoid convection damage
Minimise segregation
Minimise residual stresses
Provide location points

## Slide 5: Key Considerations – Casting Layout Design
Can the part be cast in our plant?
Feeding
  Feeder sizing is critical
    Required metal available for feeding – volume & efficiency considerations
    Modulus
  Feeding paths
Gating
  Gating sizing is critical
    Gates < 1/2 wall thickness
    Gate area to meet flow requirements - <0.5m/s through gate
    Meet requirements of fill rate – can the casting fill?
Venting!!!
  Short runs / non-fills / cold shuts
Castings Practice (2004), Campbell, J, Pg 18, Fig 2.3.1

## Slide 6: Concessions
Convention – “The way we do things”
  Experience – not always theory / scientifically based
  Established with a single objective in mind
  Established systems – e.g. pouring cups, runner systems
Some features may not be easy to implement
  Pattern / die manufacturing
  Moulding / casting constraints
  Aftercast processing
  Increasing tooling complexity
  Commercial considerations

## Slide 7: Case Studies
Aluminium Permanent Mould X 1
Ferrous Sand X 2

## Slide 8: Tanker Lid Casting – Gravity Die Casting – CA401

## Slide 9: Turbo Exhaust Collector Casting – Sand Casting - SiMo

## Slide 10: Base Casting – Sand Casting – Ni-Resist

## Slide 11: Underway

## Slide 12: Summary
The theory works and is applicable
There are difficulties with design
Implementing key requirements => better results
Still some way for us to go, but we’re on a journey!
Questions?